# Cleaning Methods

ALT Industrial Cleaner/Degreaser is designed to remove dirt and oil.  ALT has a strong affinity for oil and contaminants, and loosens them form the parts.  Most oils float to the surface, where they can be removed easily by shimming wheels/belts, absorption blankets, or vacuuming.  Turning off agitation allows solid particulates and fine metal particles to settle on the bottom, where they can be filtered off as sludge via recycling filtration systems.

Bearing Before Cleaned With ALT Degreaser

Bearing After Being Cleaned With ALT Degreaser

Heat and adequate agitation are important when using ALT’s unique formulation.  Both heat and agitation can be produced by the following methods.

# Parts Spray Washers

ALT is a significant improvement over the caustic solutions commonly used in spray washers.  At a dilution of 3% (1:30) with water, heated to 146 F, ALT effectively removes oils and greases.  Due to ALT’s low residue formula, spray nozzles stay clean from soil build-up.  No rinsing is required, single-stage washing system is practical.

# Ultrasonic Systems

In a 5% solution, ALT will remove oils, dirt, and fine metal particulates from surfaces that are agitated by ultrasonic systems.

## Heated Dip Tanks

A 5% solution of ALT heated to 145 degrees replaces all hazardous caustics and acids in submersion washing systems.  Parts washed in ALT and dried are protected from rust for 7 to 15 days.  These parts can then be coated or bonded, without further treatment.  ALT can also replace chlorinated hydrocarbons and other chemicals in a vapor degreasing tanks.  These vapor tanks can be converted to an ALT submersion system without costly equipment expenditures.  We recommend this conversion for improved agitation to ensure cleaning effectiveness.

## Oxygen and Compressed              Gas Users

ALT Industrial Cleaner/Degreaser offers a safe, simple way to clean all metal parts without fear of high residue or damage to the environment.  With proper agitation, pipe sections can be flushed clean with 3% to 5% solution.  The temperatures can range from ambient to 160 degree.  In addition, smaller hoses and parts can be submerged or sprayed.

## Rinsability

ALT Industrial Cleaner/Degreaser leaves a minimum of nonvolatile residue for corrosion protection.  In most cases this inhibitor does not have to be removed prior to subsequent metal finishing operations.  After parts are completely dry, they are protected from rust for 7 to 15 days.  These parts can then be coated or bonded, without further treatment.

## Recycling

Although oil and grease are readily “lifted” from parts by ALT Industrial Cleaner/Degreaser, the cleaning quality can deteriorate rapidly if contaminants remain in the washing systems.  In addition, recycling will improve the longevity of the cleaning solution.  Recycling systems available to remove suspended oils and extend bath life:  decanting, membranes, and micro filtration units.

Kook Je Industry

Phone 82-314797696 ( Fax 82-314797697

Email altblue@kookjeind.co.kr

## Disposal

ALT Industrial Cleaner/Degreaser can be disposed of quickly and inexpensively.  After removing excess metal particulates and tramp oil, the saturated solution can be disposed of through your sanitary sewer system when local EPA ordinances are observed.  Unlike harsher chemicals, ALT reduces the potential for regulatory penalties by the EPA and OSHA.

THROUGH PURE CHEMISTRY